## Slide 1
Advanced Physics Lab Ⅱ
2020312141 Donghun Jung
2020311441 Yujin Chon
Raman Spectroscopy for

## Slide 2
Experiment
/Results
Outline
Outline
Introduction
/Theory
Raman Spectroscopy
Graphene Phonon Mode
Graphene Raman Spectrum
Raman Spectrum
GO, RGO, Graphite
Ti2CTx
Discussion
/Conclusion

## Slide 3
Raman Spectroscopy
Raman Shift
Raman scattering is inelastic photon scattering by matter. It is called Raman shift.

## Slide 4
Raman Spectroscopy
Spectrometer
CCD

## Slide 5
Graphene
2d building block for carbon allotrpes.
* : A carbon atom bound to three atoms and forms a flat trigonal or triangular arrangement with 120ºangles between bonds

## Slide 6
Graphene Phonon Normal Mode
* : transverse anti-symmetric mode
* : transverse symmetric mode
* : out-plane symmetric mode
* : out-plane anti-symmetric mode
phonons are Raman active,
phonons are not Raman active,
Others are not Raman active but infrared active

## Slide 7
Graphene Raman Spectrum
D peak : 1330
  → It is found near the edges and defects in graphene
  Breathing modes of six-atoms ring with a defect
G peak : 1577
    → It is commonly found in graphite material
    A Stretching C-C bonding
2D peak : ~2685
  → It is always found in graphene
  There are two emitted phonons of D mode

## Slide 8
MXenes
MXenes are produced by selective etching of the A element from the MAX phases.
M : an early transition metal
A : A-group(mostly 13, 14 groups)
X : C or N
Ex)

## Slide 9
GO, RGO, Graphite – Experiment result

## Slide 10
GO, RGO, Graphite

## Slide 11
Ti2CTx – Experiment Result

## Slide 12
Ti2CTx
ω3
ω2
ω1
D
G
ω1 : 279, ω3 : 615
→ vibration mode of Ti, C and surface
terminating functional groups(Ti-O, Ti-C, Ti-OH)
ω2 : 420
→ vibration mode of Ti and Al in MAX phase
D peak : 1326
→ breathing mode of six-atoms rings with a defect
G peak : 1574
→ a stretching C-C bonding

## Slide 13
Defects
(Crystallographic) Defects are…
all the interruptions of regular patterns in crystalline solids.
In this experiment, defects occur due to extensive oxidation and due to the restoration of structure. The observable results in the Raman spectroscopy of GR, GO, RGO caused by defects are …
D, D, D+D peak appear.
All peaks are broaden.
increases.

## Slide 14
Defects and Crystal Size
are known to be related to crystal size , defect distance . The ratio of its intensity to that of the G peak varied inversely with and .
[nm]

## Slide 15
Conclusion

## Slide 16
References
[1] Ferrari, A., Basko, D. Raman spectroscopy as a versatile tool for studying the properties of graphene. Nature Nanotech 8, 235–246 (2013)
[2] Lim, Gim Pao et al. “Synthesis, characterization and biophysical evaluation of the 2D Ti2CTx MXene using 3D spheroid-type cultures.” Ceramics International (2021)
[3] Alhwaige, Almahdi A. et al. “Interactions, morphology and thermal stability of graphene-oxide reinforced polymer aerogels derived from star-like telechelic aldehyde-terminal benzoxazine resin.” RSC Advances 5 (2015)
[4] Hidayah, N. M. S. et al. “Comparison on graphite, graphene oxide and reduced graphene oxide: Synthesis and characterization.” (2017)
[5] Iqbal A, Hamdan NM. Investigation and Optimization of Mxene Functionalized Mesoporous Titania Films as Efficient Photoelectrodes. Materials. (2021)

## Slide 17
Thank you