## Slide 1
Advanced Physics Lab Ⅱ
2020312141 Donghun Jung
2020311441 Yujin Chon
Raman Spectroscopy for

## Slide 2
Experiment
/Results
Outline
Outline
Intro
/Theory
Raman Spectroscopy
Graphene Phonon Mode
Raman Spectrum
GO, RGO, Graphite
Ti2CTx
Discussion
/Conclusion

## Slide 3
Raman Spectroscopy
Raman Shift
Raman scattering is inelastic photon scattering by matter. It is called Raman shift.

## Slide 4
Raman Spectroscopy
Spectrometer
CCD

## Slide 5
Graphene Phonon Mode
* : transverse anti-symmetric mode
* : transverse symmetric mode
* : out-plane symmetric mode
* : out-plane anti-symmetric mode
phonons are Raman active,
phonons are not Raman active,
Others are not Raman active but infrared active

## Slide 6
Graphene Raman Spectrum
D peak : ~1330
  → It is found near the edges and defects in graphene
G peak : ~1577
    → It is commonly found in graphite material
2D peak : ~2685
  → There are two emitted phonons of D mode

## Slide 7
GO, RGO, Graphite

## Slide 8
GO, RGO, Graphite

## Slide 9
Ti2CTx

## Slide 10
Raman Spectrum

## Slide 11
Conclusion

## Slide 12
References
[1]
[2]

## Slide 13
Thank you